## Slide 1
  MW-modulated Photoluminescence
  Imaging of 2DEG magnetoplasmons
  B.M. Ashkinadze
Physics Department, Technion-Israel Institute
of Technology, Haifa 32000, Israel

## Slide 2
OUTLINE
Photoluminescence of MDQW and HJs containing a 2DEG - different physical mechanisms
2D-electron cyclotron (magnetoplasma) resonance - microwave absorption by a 2DEG
Mw-modulated Photoluminescence and Optically detected CR-resonance : - hot 2DEG, phonon wind and “heating” of holes
2D-plasmon imaging - spatially-distributed mw-field affecting the 2DEG

## Slide 3
GaAs/AlGaAs modulation-doped heterostructures
n 2D = (0.2-3)x1011 cm-2
~ (1- 25)x106 cm2/ Vs (at TL< 2 K)
Heterojunction, HJ [ d > 500 Ǻ]
Quantum well (MDQW) [d~100-500 Ǻ]
GaAs Eg=1.519 eV
AlxGa1-xAs Eg=1.8 eV (x=0.18-0.33)
Si d- doping.
2D-electrons
(L~100-200Ǻ)
d
GaAs layer width
Samples were grown by L. N. Pfeiffer and V. Umansky
L <(1 -1.5) x10-4 cm
Intrinsic Photoluminescence:
spectrum - J(Em)
intensity - J
under mw irradiation
Laser Light: hn =1.56 - 2.0 eV
a -1 > 10-4 cm ~ L
Very low excitation:
PLaser < 50 mW ( IL~ 30 mW/cm2)
dn ~ dp (<107cm-2) << n2D

## Slide 4
Drift of the photoexcited holes away
from the interface into the flat band
region
HJ built-in E
Exciton PL
in a single HJ
2De-hole PL
Photoluminescence in high quality heterostrustures
light illumination
2DEG
Si+
EF
E gap~1.8 eV
QW 25nm
GaAs
Al0.33Ga0.67As
Al0.33Ga0.67As

## Slide 5
PL spectrum of the 2De-h radiative recombination
Eg
E
EF
EF Te
ee
fe
dn ~ dp <<n2D
eh
fh ? “Th”
tR
t e
at te << t R
Th =TL
at t R << te
“Th” >TL
Direct optical transitions:

## Slide 6
2DEG PL in quantum wells B=0
2DEG
2De-h PL
MDQW-width and n2d variations
optical depletion:
n2De decreases
Effect of mw-radiation on
the 2De-hole PL spectrum
< Eg (AlGaAs)
EL =1.96 eV> Eg (AlGaAs)

## Slide 7
n ~2
filling factor:
PL in MD QW & HJ: spectral evolution under magnetic field
MDQW, 20 nm
n2D= 1011 cm-2
Photon energy
Exciton
2De-hole PL
Exciton to 2De-h PL changeover at n ~ 2 (4)
(+optical depletion)
single HJ
T=2 K

## Slide 8
l/4
Pmw
E
Pmw- P absmw
LOCK-IN
Gunn-Diode
SPECTRO-
METER
PM
B (0-1T)
Laser light (1.56 & 1.96 eV)
MW
DETECTOR
CIRCULATOR
ATTENUATOR
T= 2-300 K
cw
p-i-n
modulator
Chopper
Experiment
f =33-37 GHz, l~ 8mm, TE10 mode
mw absorption
PL & Mw-modulated PL

## Slide 9
Electron Cyclotron Resonance - mw absorption
Drude CR-line shape
negligible mw reflection (“radiative broadening”)
At increased Pmw the CR-line broadens
2DEG: high n2D - a magnetoplasma shift
m* = 0.066 me
tm ~110 ps
m~2x106
Mw-absorption
bulk photoexcited GaAs
low ne ~ 1012 cm-3
n2D0=2.6 x 1011cm2
n2D =1 x 1011cm2
mesa 0.7 mm, HJ
+ HeNe laser light
TL =20K
TL =2K
m=2.4x106 cm2/Vs
Pmw > 0.1 mW
Te~6K, TL =2K
DMPR
(dimensional magne-
toplasma resonance)
MOCVD-grown
Pmw~1 mW

## Slide 10
Electron temperature, Te increases
2DEG under increased microwave radiation
Power loss per electron versus Te
M. E. Daniels, B. K. Ridley, S.S.Electronics.32, 1207 (1989).
N.Balkan et.al., Semicond. Sci. Technol.17(2002) 18–29
Pabs (at CR) : #1x1 mm, n2D = 1011cm-2 , Ne= 109 el
Pabs = ~ 10% Pin ~10-5 W (at Pin =0.1 mW )
Pabs / Ne ~ 10-14 W / el TRe ~5-10 K
10-15 W/el , Te ~ 5 K
10-14 W/el , Te ~ 10 K
Low-energy ballistically propagated acoustic phonons (free path > sample size)
(dc-current exp.)
The mw-heated 2DEG emits phonons

## Slide 11
Microwave-induced PL change
Te, “Th”
2 , 2.5 K
3, 4.5 K
8, 18 K
“Th“ > Te ?!
Te and “Th” reaches
maximuma at e-CR
Primary effect is a
2D-electron mw-heating
Bc
2D-electron heating leads to energy redistribution of photoexcited holes!
via nonequilibrium phonons emitted by warm 2DEG (2De and holes are spatially separated!)
Spectra at B=0
2DEG
B
mw

## Slide 12
NA phonons
EL
A net hole energy relaxation rate decreases
due to “hole heating” mediated by NA phonons
no effect
Direct effect of the increased Te
To clarify the physical mechanisms
that govern the mw-induced effects:
The hole-energy distribution is governed by
the competition of two processes:
hole recombination with the 2DEG and
hole-energy relaxation due to inelastic
scattering by acoustic phonons.
light excitation
(An indirect 2DEG-hole interaction)
Transient dynamics
Te relaxation time < 10-9 s
Nph ~ 10 -7 - 10-8 s
expected
observed

## Slide 13
Transient dynamics of mw-modulated PL (under short mw-pulses)
Time-resolved (2 ns gate) PL spectra
The transient PL intensity
(Em =1.524 eV, B=0.085 T, Pmw =0.1 - 1 mW)
The PL spectrum has not recovered
after 15 ns delay time
Overshoots and a long decay time
after the mw pulse terminates
PL intensity relaxes much longer than the leading and trailing mw-pulse edges (~3-5 ns)!
Hole-energy relaxation time ~ Nonequilibrium acoustic phonon lifetime ~10 ns

## Slide 14
Interaction of free excitons with 2DEG in a single HJ
FE
2De-hole PL
Light
2DEG
EF
E0
z=d
hole drift in EHJ
z=0
exciton diffusion (drift)
Excitons dissociate into 2De and 3D-hole
near the 2DEG (rate S2).
2DEG mw-heating causes a remarkable change in the exciton PL (for HJ)
PL changeover: a steep S2 increase at filling factor n < 2
The exciton-2DEG dynamics is affected by NA phonon flux :
The excitons are repelled from hot 2DEG {nex(d) decreases}

## Slide 15
Optically detected FIR 2D-e cyclotron resonance in a single HJ
No 2DEG-PL spectral shift:
Negligible FIR-induced
n2D-change on the lowest LL
S2 nex decreases
(resulting in the decreased p)
PFIR ~2 mW/cm-2
--- Drude line for m=3x106 cm2/Vs
FIR-heated 2DEG emits
a phonon flux (wind) exerting
a force on the exciton.
The excitons “are repelled”
from the 2DEG
LL0
LL1
10.43 meV
(L. Keldysh, 1976)
ODR mechanism:
Line shape for
ODR = FIR CR absorption
Radiative broadening (l<<a)

## Slide 16
2D-e DMPR (mw- CR) detected by the exciton PL in a single HJ
Free excitons respond
to mw-heating of the 2DEG !
Jex increases (x1.5-2)
and then decreases
J2De-h decreases
FE spectrum broadens
Pmw
Absorption of the NA-phonons by the excitons results in:
1. repelling the excitons from
the 2DEG (Jex increases )
2. exciton heating (E. Ivchenko et.,al. Solid State, Physics 30, 1161, 1988)
B=0
Exciton PL intensity , Jex
mw-pulses: 10-5 s
10-4s
3 PL gate positions
The electrons cooled down,
no phonon wind
The long-lived FE PL hysteresis
- decreased n2D
n2D=2.6x 1011cm-2 (0.7mm mesa)
Jex (Em=1.515 eV)
B, T
B, T
lowest IL
Jex at 1.515 eV
Jex vs Pmw
P mw1
P mw2 >
Remarkable mw-ODR line shape
Hysteresis at Pmw > 1 mW
Jex(Pmw=0)

## Slide 17
Dynamics of mw-induced exciton PL modulation (single HJ)
FE exciton heating under 2DEG mw-heating:
Absorption of non-equillibrium phonons
GaAs/AlGaAs HJ, n2D=1.4x1011cm-2
Mw-induced PL modulation lasts ~20 ns
The strongest mw- modulation - at high PL energies

## Slide 18
Spatially resolved mw-modulated PL
as a probe of the local microwave field acting the 2DEG
Spatially resolved PL
(1mm2 excitation spot)
D y  10 mm
DEphoton  0.1 meV
Imaging mw-induced PL spectroscopy
Eloc(y)
PL intensity at dEmon : Jmon = f( Te ) = f (|Eloc|2 )
Spatial n2DEG and Te –distribution (in-2DEG plane)
Local electron temperature: “hot” and “cold” spots
+Emw
y
GAs+2DEG
mw
y
x
4mm
7.2 mm
B
Ey
2DEG
d
L
CCD image
Photon energy
y
Spatially integrated PL
(0.1mm2 excitation spot)
Jmon (y) ~ |Eloc(y)|2
(for HJ PL)
Notes: 18

## Slide 19
Standing wave resonances: (lmp /2) j =d
d
Emw (y)
j=1
j=2
j=3
PL int. J
MDQW 20nm
n2D=
1011cm-2
2x1010 cm-2
2x1010cm-2
Single HJ
PL patterns induced by MW
Inc(ident
Spatial PL inhomogenity is due to
Excitation of confined magnetoplasmons
Ballistically -propagated phonons
no MW
B=0
B=0
q=2p/lmp = j (p/d)
Local electric field mapping

## Slide 20: Local mw-field reconstruction:
B, n2D and f dependencies fit qualitatively
to magnetoplasmon dispersion relation:
Patterns are independent
of mw power !
from the high-energy
PL intensity
IPL
Patterns depend on n2D and B
The direct observation of magnetoplasmon
modes excited by mw in a laterally confined 2DEG
The mw-field affecting the 2DEG is spatially inhomogeneous
JPL(y)  Te  |Emp|2

## Slide 21
Conclusions
2De-hole (or excitonic) photoluminescence is a sensitive probe of the microwave induced effects in the heterostructures containing a 2DEG
Non-equilibrium acoustic phonon flux emitted by the warm 2DEG plays an important role in the mw-induced phenomena. These phonons leading to a hole (exciton) “heating”, are the underlying agent of the PL spectral changes, in particular, of the optically detected 2D-e CR-resonance.
In the HJ, the excitonic and 2De-h photoluminescence are in dynamical equilibrium. Such an equilibrium can be controlled by the phonon wind from the warm 2DEG
Spatially resolved photoluminescence maps the spatial non-uniformity of the internal microwave field (as well as the 2DEG density) and is used to image magnetoplasmons excited by a microwave radiation.
Many thanks for collaboration: Ilya Baskin, E. Cohen, E. Linder, G. Bartsch, D. Yakovlev
Thank you for attention

## Slide 22
Direct optical transitions due to recombination of low-density photoholes in the valence band (v.b.) and 2D electrons in the conduction band (c.b.).
(b) A schematic description of the Hall bar and the spatially resolved photoluminescence experiment

## Slide 23
B.M. Ashkinadze, E. Linder, V. Umansky
Dimensional magnetoplasma resonance detected by free-exciton
photoluminescence in modulation-doped GaAs/AlxGa1-xAs heterojunctions
Phys. Rev. B 62, 10310, 2000
B.M. Ashkinadze, V. Voznyy, E. Linder, E. Cohen, L.N.Pfeiffer
Photoluminescence hysteresis of the optically detected cyclotron-like resonance of a 2DEG
Phys. Rev. B 64, 161306, 2001
B.M. Ashkinadze, V. Voznyy, E. Cohen, A. Ron, V. Umansky Condensation of bulk excitons on a magnetized 2DEG in modulation-doped heterojunctions Phys. Rev. B 65, 073311, 2002
B.M. Ashkinadze, E. Linder, E. Cohen, V. Rudenkov, P. Christianen, L.N.Pfeiffer Exciton to two-dimensional electron-hole photoluminescence transitions driven by the quantum Hall effect . Phys. Rev. B 72, 075332, 2005
B.M. Ashkinadze, E. Linder, E. Cohen, L.N.Pfeiffer Microwave-modulated photoluminescence of a two-dimensional electron gas Phys. Rev. B 74, 245310, 2006
I. Baskin, B.M. Ashkinadze, E. Cohen, L.N.Pfeiffer Microwave-induced photoluminescence modulation and optically detected resonances due to a 2DEG in a heterostructure Phys. Rev. B 78, 195318, 2008
I. Baskin, B.M. Ashkinadze, E. Cohen, L.N.Pfeiffer Imaging magnetoplasmons excited in a two-dimensional electron gas Phys. Rev. B 84, 041305, 2011
G. Bartsch, C. Zens, B.M. Ashkinadze, D.R. Yakovlev, M. Bayer Optically detected far-infrared cyclotron resonance of two-dimensional electrons in a single GaAs/(Al,Ga) As heterojunction Phys. Rev. B 87, 085316, 2013
I. Baskin, B.M. Ashkinadze, E. Cohen, L.N.Pfeiffer Luminescence flashes induced by microwave radiation in undoped GaAs QWs Phys. Rev. B 79, 195325, 2009

## Slide 24
Exciton – 2DEG PL transition (model )
at n >2 - low S2 _ No 2DEG-hole PL
at n < 2 - high S2 – PL changeover
V1 – potential well for exciton
V2 = Vkin + V 2De-3h
D=100cm2sec
tex=10-9sec
S1=103 cm/sec
Approaching to the 2DEG, excitons dissociate into 2De and 3D-hole with a rate S2 that depends on B
Phys. Rev. B 72, 075332, 2005
Distant interaction of hot 2DEG with excitons : Non-equilibrium phonons affect the exciton-2DEG dynamics and S2 reduces

## Slide 25
Nonlinear Dimensional Magnetoplasma
Resonance (DMPCR)
As Pmw increases - DMPCR shifts to higher B:
2DEG density decreases with Te (mw-power)
B. Ashkinadze, V. Yudson, PRL83, 812, 1999
2DEG density varies under high mw-power
EF
Classical nonlinear
oscillator
2DEG under increased microwave radiation (c)
(nonlinear coefficient b)

## Slide 26
sample
Longitudinal modes
Magnetoplasmon dispersion
At d <<L, qx~ p/L << qy ~ p/W
qy
qx
L
d
Emw

## Slide 27
Direct optical transitions due to recombination of low-density photoholes in the valence band (v.b.) and 2D electrons in the conduction band (c.b.).
(b) A schematic description of the Hall bar and the spatially resolved photoluminescence experiment