## Slide 1
Leonid Ponomarenko
Graphene Superlattices

l
QT2DS, Luchon (France), 26/05/15

## Slide 2: Collaboration and Support
Fabrication (Manchester):
Roman Gorbachev, Greg Auton, Andrey Kretinin, Freddie Withers
The project lead by Andre Geim and Kostya Novoselov
Transport measurements and AFM (Manchester):
Artem Mishchenko, Geliang Yu, Colin Woods, Roshan Krishna Kumar
High magnetic fields (Grenoble, CNRS)
Marek Potemski, Benjamin Piot
Theory (Lancaster):
Vladimir Falko, John Wallbank, Martin Mucha-Kruczynski

## Slide 3: Outline
Graphene: quick introduction
Graphene heterostructures
Graphene Superlattices
Hofstadter butterfly in transport & quantum capacitance
Commensurate-incommensurate transition
Valley Hall Effect

## Slide 4
Band Structure and Field Effect
P. Wallace, Phys. Rev. 71, 622 (1947)
Geim & Novoselov, Science 2004
Mechanical exfoliation (“Sticky tape” method)
SiO2
Si
graphene
Hexagonal lattice, A-B sublattice symmetry (= inversion symmetry)

## Slide 5
Band Structure and Field Effect
Geim & Novoselov, Science 2004
Mechanical exfoliation (“Sticky tape” method)
SiO2
Si
graphene
B – magnetic field n – carrier density
µ - mobility
10 000 cm2/Vs (on SiO2)
1 000 000 cm2/Vs (suspended, 4 K)

## Slide 6: Graphene Heterostructures
Boron nitride substrates for high-quality graphene electronics
C. R. Dean et al. Nature Nano 5, 722 (2010)
One order improvement in mobility.
Dean et al., Nature Phys. (2011)
Fractional Quantum Hall Effect

## Slide 7
Fullerene-like molecule B12N12
Different forms of Boron Nitride
Hexagonal – “white graphite”
BN nanotubes
Cubic – almost as hard as diamond
BN: insulator with gap 5.8 eV
K. Watanabe et al, Nature Materials 2004.
Graphene
Boron Nitride
a = 2.504 A, c = 6.661 A
a = 2.462 A, c = 6.708 A

## Slide 8
Multi-Layer Structures
Graphene
Boron-Nitride
NbSe2
GraFane
Graphane
MoS2
Van der Waals heterostructures. Geim & Grigorieva, NATURE (2013)

## Slide 9
Dry-peel transfer

## Slide 10
Mobility and Mean Free Path

## Slide 11
Mobility and Mean Free Path
The width of the Hall bar is 2 m
At low temperatures the MFP is limited by the size of the device

## Slide 12
2 nm
everything covered
with contamination
TEM
2 nm
occasional
10 nm scale
patches
so much contamination  BUBBLES
optics
SEM
20 m
0.5 m
AFM
AFM
Bubbles

## Slide 13
Manchester, Nature Materials 2012
10 m
SEM
TEM
chemical
analysis
NO CONTAMINATION LAYER
at the interface
between graphene & hBN
graphene-hBN interface in TEM
Focused ion beam (FIB) milling + STEM
Slices 20-70 nm thick

## Slide 14
moiré patterns: graphene on hBN
Yankowitz et al, Nature Phys 2012
Xue et al, Nature Mat 2011; Decker et al, Nanolett 2011
6.0 nm
periodicity =2.4 nm
11.5 nm

l
THEORY:
Steve Louie‘s group
Nature Phys 2008, PRL 2008
Francois Peeters’ group
PRB 2010-2012
Burset et al, PRB 2011
Ortix et al, PRB 2012
Kindermann et al, PRB 2012
Fal’ko et al, PRB 2013
and SOME MORE
1.8% lattice mismatch
STM

## Slide 15
moiré patterns: graphene on hBN
Yankowitz et al, Nature Phys 2012
6.0 nm
periodicity =2.4 nm
11.5 nm

l
New Dirac points
generated
at the edges of
the superlattice
Brillouin zone
for short periods,
gaps lie at
too high energies

## Slide 16
can we probe in transport?
Yankowitz et al, Nature Phys 2012
6.0 nm
periodicity =2.4 nm
11.5 nm
<2 degrees
accessible by
the field effect
for short periods,
gaps lie at
too high energies
“invisible”
for transport
measurements
need moiré
like this

## Slide 17
ambient CAFM:
moiré in graphene on BN
with 12 nm period
specially aligned graphene devices

## Slide 18
secondary Dirac points
new neutrality points @0.2-0.35 eV
second generation
Dirac fermions
electron-like orbits for
strong hole doping and vice versa
specially aligned graphene devices
n~3x1012 cm-2,  = 13 nm, (A = 150 nm2)
4 electrons/u.c.
Ponomarenko et al. Nature (2013)

## Slide 19
what happen in magnetic field?
Two competing lengthscales: a : lattice periodicity
lB : magnetic length
Duglas F. Hofstadter, Phys. Rev. B 14, 2239 (1976)
/0

0
1
Energy levels develop fractal structure when magnetic length is of the order of the lattice period
flux quanta per unit cell
a ≈ 0.25 nm ⇒ B ≈ 104 T
graphene:
graphene/BN superlattice:
 ≈ 14 nm A ≈ 170 nm2
B ≈ 24 T (/0 = 1)

## Slide 20
Tracing gaps in B and n
/0

0
1
/0
n/n0
0
1
Hofstadter’s energy spectrum
ℤ
gaps are constrained to linear trajectories in the B-n diagram:
Wannier diagram
Phys. Status Solidi 88, 757 (1978)
n/n0 – normalised density (n0 = 4/A, where A is the area of supercell)

## Slide 21
Magnetotransport measurements
Some of the features of Hofstadter’s energy spectrum are seen in magnetotransport
Ponomarenko et al. Nature (2013)
“Landau levels” fanning from the secondary DP

## Slide 22
Magnetotransport measurements
Some of the features of Hofstadter’s energy spectrum are seen in magnetotransport
Enhanced conductivity, periodic in 1/B
Ponomarenko et al. Nature (2013)

## Slide 23: Capacitance Measurements
L.A.Ponomarenko et al,
PRL 105 136801 (2010)
Simple and reliable technique for studying details of the band structure
density of states
“geometrical” capacitance

## Slide 24
Signatures of Hofstadter’s butterfly
Capacitance measurements: density of states can be probed directly
G.L.Yu et al. Nature Physics 10, 525 (2014)
Black – Landau fan (4x degenerate)
Blue – Landau fan (degeneracy lifted, QHFM)
Green – “Landau levels” from secondary DPs
Red – gaps in Hofstadter spectrum
Dark colours correspond to low DOS

## Slide 25
Commensurate-incommensurate transition in graphene on hBN
λ = 8nm
λ = 14nm
Resistance
Young’s modulus
Woods et al., Nature Phys., 10, 2014, 451.

## Slide 26
Two types of G/hBN superlattices
Incommensurate:
Not aligned
No global gap
Commensurate:
Global A/B asymmetry
Global gap
Woods et al., Nature Phys., 10, 2014, 451.
Ponomarenko et al., Nature, 497, 2013, 594.

## Slide 27
Massive Dirac Fermions in
van der Waals Heterostructure
Hunt et al., Science., 340, 1427 (2013)
A gap opens at the Dirac point in aligned structures,
Chen et al., Nature Comm. 5, 4461 (2014)

## Slide 28
Berry Curvature
The Berry curvature is an intrinsic property of the bend structure: if is the eigenstate of the Hamiltonian , then the Berry curvature (density) is:
Magnetic flux
(some key properties)
for the system with both inversion and time reversal symmetries
is the local quantity (in k-space)
is observable (gauge invariant)
affects electron dynamics, for example, group velocity
Relation to the Berry phase along a closed path C:
, where S is the surface enclosed by C
Anomalous velocity

## Slide 29
Berry curvature in gapped graphene
Xiao D., Yao W., Niu Q.,
PRL, 99, 2007, 236809.
Different A and B sublattices = Broken inversion symmetry
hot spots at K and K’
Time reversal symmetry requires
B = 0,

## Slide 30
Berry curvature in gapped graphene:
nonlocal measurements
Gorbachev et al., Science, 346, 2014, 448.
B = 0T, T = 20K
Berry curvature hot
spots
Valley Hall effect: voltage applied across the device gives rise to counter-propagating streams of carriers in two valleys. A reverse process creates the electric field in remote regions.

## Slide 31
Nonlocal measurements:
carrier density dependence
Gorbachev et al., Science, 346, 2014, 448.
B = 0T, T = 20K

## Slide 32
Nonlocal measurements:
length dependence
Gorbachev et al., Science, 346, 2014, 448.
B = 0T, T = 20K
Nonlocal signal decays exponentially with increasing L
anomalous contribution to ρxx observed in the bend geometry
ξ ≈ 1 μm
L =
7 μm
10 devices,
20 K

## Slide 33: Conclusions
Graphene superlattice is an excellent example of “band structure engineering” and creating artificial structures with on demand properties (simply by controlling the orientation of graphene with respect to the properly chosen substrate)
Hofstadter butterfly has been finally observed (almost 40 years after its prediction)
Thank you!
Valley Hall effect observed in gapped graphene in zero field