## Slide 1: CVD graphene for quantum metrology
R. Ribeiro-Palau
Laboratoire National de Métrologie et d’Essais
(French National Metrology and Testing Laboratory)

## Slide 2: Electrical resistance standard
Quantum Hall resistance in GaAs/AlGaAs has been the practical electrical resistance standard of the SI since 1990
Typical accuracy of DRH/RH≈10-9
in GaAs/AlGaAs devices
- 400 mm wide Hall bar
- I ≤40 mA
- B ≥ 9 T
- T ≤ 1.3 K
Practical?
Applying a magnetic field
RH=RK/2=h/2e2
kilogram standard

## Slide 3: Outline
Why to use graphene as an electrical resistance standard?
Is graphene truly better than GaAs/AlGaAs?
Our approach: CVD on SiC
Highly accurate experiments: B, T, I space

## Slide 4: Graphene as an electrical resistance standard
DE/kBT > 100
To minimize thermal activation between Landau levels
DE >> kBT
More precisely, to obtain 1 part in 109 precision:
First Landau levels spacing
Graphene advantages:
@ 2 K
New generation of electrical resistance standards:
GaAs
Monolayer graphene
- Lower magnetic field (B<5 T)
- Higher temperature (T>4 K)
- High operation current (I >100 µA)
Transportable coils
Helium free cryostats
Commercial resistance bridge

## Slide 5: Graphene QHRS timeline
2005
2014
2009
Observation of the QHE in graphene
K. Novoselov et al., Nature (2005)
Y. Zhang et al., Nature (2005)
First accurate measurements
A. J. M. Giesbers et al., APL (2009)
2010
A. Tzalenchuk et al., Nature Nano (2010)
Highly accurate measurements
DRH/RH=9x10-11
B= 14 T
T= 300 mK
Not yet competitive with GaAs-based quantum resistance standards
T. J. B. M. Janssen et al., New J. of Phys. and Metrologia (2011)
2015
2011
DRH/RH=15x10-6
B= 14 T
T= 300 mK
… ?
 | Large size (10000 mm2) | High mobility (>5000 cm2V-1s-1) | Low carrier density (<2x1011 cm-2) | Reproducible result
Mechanical exfoliation | ✗ | ✓ | ✓ | ✗
SiC sublimation | ✓ | ✓ | ✗ | ✗
CVD | ✓ | ✓ | ? | ?
2013
Lafont F., Ribeiro-Palau R. et al., PRB (2014)
Anomalous dissipation mechanism in CVD graphene

## Slide 6: Chemical vapor deposition on SiC
Horizontal hot-wall CVD reactor designed for SiC epitaxy
P = 800 mbar
T = 1550 °C
Carrier gas:
Hydrogen/Argon
(23 % H)
Precursor
C3H8
Semi-insulating 0.16° off-axis 6H-SiC substrate
SiC
Graphene
C
More details in: A. Michon et al., APL (2010)

## Slide 7: Chemical vapor deposition on SiC
ARPES
MLG ns≈1x1013 cm-2
BLG ns≈3x1012 cm-2
Atomic Force Microscopy
Low energy electron microscopy
More details in:
Jabakhanji et al. PRB (2014)

## Slide 8: Chemical vapor deposition on SiC
ARPES
MLG ns≈1x1013 cm-2
BLG ns≈3x1012 cm-2
Low contact resistance (< 1 W)
essential in accurate measurements
Hall bar of 420 μm x 100 μm
500°C annealing + P(MMA-MAA)/ZEP520A
(no illumination)
Lara-Avila S. et al., Adv. Mat. (2011)
ns=3.2x1011 cm-2
µ=3800 cm2V-1s-1
Chemical gate

## Slide 9
F. Lafont, R. Ribeiro-Palau et al., Nature Comms. (2015)
Longitudinal resistance or quantization parameter
Coupling factor:
-0.67
To preserve 1x10-9 accuracy
Rxx≤ 20 mW
Accurate Hall resistance measurements
T=1.3 K
Resistance quantization
GaAs/AlGaAs
Graphene
100 W
wire resistor
rGaAs
Indirect comparisons of RH-G with the resistance of a GaAs-QHRS (LEP514) via an intermediate room-temperature 100 W resistor, using a cryogenic current comparator bridge.
rGraph
1s.d.
ns=3.2x1011 cm-2

## Slide 10
Longitudinal resistance or quantization parameter
Coupling factor:
-0.67
To preserve 1x10-9 accuracy
Rxx≤ 20 mW
Accurate Hall resistance measurements
10-9 accuracy under the same conditions as GaAs QHRS
10-9 accuracy over a magnetic field range of 9 T
(in GaAs/AlGaAs samples <2 T)
T=1.3 K
F. Lafont, R. Ribeiro-Palau et al., Nature Comms. (2015)
Resistance quantization
1s.d.
Quantization regime does not correspond to n=2 (calculated from ns)
ns=3.2x1011 cm-2

## Slide 11
Variable Range Hopping mechanism
Resistance quantization
4 K
40 K
(7 T- 19 T)
Possible linear increase of the density with magnetic field
ns=3.2x1011 cm-2

## Slide 12
Breakdown current
Alexander-Webber et al. PRL (2013)
Graphene from sublimation of SiC
ns~6.5x1011 cm-2
ns=3.2x1011 cm-2
x 2
Maximum of current is found at n integer
Breakdown current in GaAs/AlGaAs
Jeckelmann et al. IEEE Trans. Instrum. Meas. (2001)

## Slide 13: Chemical vapor deposition on SiC
Horizontal hot-wall CVD reactor designed for SiC epitaxy
P = 800 mbar
T = 1550 °C
Carrier gas:
Hydrogen/Argon
(44 % H)
Precursor
C3H8
Semi-insulating 0.16° off-axis 6H-SiC substrate
SiC
Graphene
C
More details in: A. Michon et al., APL (2010)

## Slide 14: Chemical vapor deposition on SiC
Hall bar of 420 μm x 100 μm
500°C annealing + P(MMA-MAA)/ZEP520A
(no illumination)
Lara-Avila S. et al., Adv. Mat. (2011)
Chemical gate
ns≈1.8×1011 cm-2
μ≈9 400 cm2V-1s-1

## Slide 15: Quantum Hall effect in CVD graphene on SiC
Graphene has a n=2 plateau, at least, 6 times larger than GaAs/AlGaAs

## Slide 16: Breakdown current
Breakdown current in GaAs/AlGaAs
Jeckelmann et al. IEEE Trans. Instrum. Meas. (2001)
Critical current increase linearly with the magnetic field
Graphene from sublimation of SiC
Alexander-Webber et al. PRL (2013)
ns~1x1011 cm-2
ns=1.8x1011 cm-2

## Slide 17: Temperature effects
ns=1.8x1011 cm-2
Highest breakdown current
Highest temperature
Quantization range

## Slide 18: Graphene vs GaAs/AlGaAs

## Slide 19: Conclusions
Graphene will replace GaAs/AlGaAs from the national metrology institutes
It will be highly involved in the dissemination of practical standards towards the industry.
It will help in the redefinition of the kilogram.
What is the origin of the shift of n=2 ?

## Slide 20: Quantum Metrology group - LNE
Thanks for your attention
In collaboration with:
W. Poirier
F. Schopfer
J. Brun-Picard
F. Lafont
D. Leprat
A. Michon (CRHEA-Valbonne, France)
D. Kazazis (LPN-Orsay, France)
B. Jouault (L2C- Montpellier, France)

## Slide 21
“It will be ironic if massless Dirac fermions were involved in a new definition of the Kilogram”
Mass appeal,
Editorial Nature Nanotech (2010).