## Slide 1
Sergei Studenikin, Geof Aers, and Andy Sachrajda
National Research Council of Canada, Ottawa, Canada
Electron effective mass in an ultra-high mobility GaAs/AlGaAs quantum well from MIRO and EPR experiment on DPPH
Q. Shi, and M. A. Zudov
School of Physics and Astronomy, University of Minnesota, Minneapolis, Minnesota, USA
L. N. Pfeiffer, and K. W. West
Department of Electrical Engineering, Princeton University, Princeton, New Jersey, USA
Notes: Electron effective mass in an ultra-high mobility GaAs/AlGaAs quantum well from MIRO and EPR experiment on DPPH
MIROs as a presize tool to study electron effective mass
Joan Miró (1893-1983) - famous Spanish artist

## Slide 2
Three first MIRO/ZRS papers: number of scitations per year

## Slide 3
Joan Miró (1893-1983)
First time use of “MIRO”

## Slide 4
Niko Pirosmani (1862-1918)

## Slide 5
Electron effective mass in an ultra-high mobility GaAs/AlGaAs quantum
well from MIRO and DPPH EPR experiment
Outline
Introduction: methods for m*-measurements
Sample and Experimental setup
B calibration with DPPH in 5-70 mT range
m*MIRO measurement
Conclusions
Notes: .

## Slide 6
Why it is interesting to precisely measure m*?
m*0 is a band parameter
m* (w, Ei, B, ….) is sensitive to details
m* is sensitive to e-e interactions
Can MIRO be used as a precise tool for m* ?
What kind of m* is deduced from MIRO ?
Notes: m* engineering …. What matters how precisely and reliably we measure
Can MIRO be used to precisely measure m* in small fields?

## Slide 7
Known methods to measure 2DEG m*: FIR cyclotron resonance
In FIR experiments m* is affected by high B, SdH, plasmons
Important comment: CR resonance is not effected by e-e interactions
Kohn’s theorem - Phys. Rev. 123, 1242 (1961)
S.S. et al. Phys. E 34, 73 (2006).
Maan et al. APL 40, 609 (1982).

## Slide 8
Remark: CR cannot be reliably measured in high-mobility 2DEG at MW
Calculated reflection/absorbtion by ideal 2DEG
A cavity measurements of absorption in a 1mm 2DEG strip
CR on photo-excited electrons in bulk GaAs by B.Ashkinadze PRB 52, 17165 (1995)
S.S., et al., Phys. Rev. B 76, 165321 (2007)
(1)
(2)
(3)
Notes: Unfortunately we cannot faithfully measure CR in so high-mobility samples in low B

## Slide 9
Known methods to measure m*: magneto-plasmon resonance
m*=0.070 m0
Vasiliadou, Miller, Heitmann, Weiss, von Klitzing, PRB 48, 17145 (1993)
n=2.3x1011 cm-2, m=1.2x106 cm2/Vs
Notes: Retardation effects may effect MPR position
CR simply does not work in such high mobility samples

## Slide 10
Magneto-plasmon resonance experiment on high-mobility samples
Hatke, Zudov, Watson, Manfra, Pfeiffer, West, PRB 87, 161307(R) (2013)
n=2.7x1011 cm-2 , m=1.3x107 cm2/Vs
=e/2

## Slide 11
Magneto-plasmon resonance in MW absorption on a high-mobility sample
w=0.8 mm
n=1.8x1011 cm-2
m=3x106 cm2/Vs
m*=0.068 m0
m*  0.068 m0
FEDORYCH, STUDENIKIN, MOREAU, POTEMSKI, SAKU, HIRAYAMA, Int. J. Mod. Phys. B 23, 2698 (2009).

## Slide 12
Effective mass m* from T-dependence of Shubnikov – de Haas oscillations
BUT:
SdH m* measurements can be affected by side effects…
M. Zudov (not published)

## Slide 13
Effective mass m* from SdH oscillations: side effects
Possible technical issues:
SdH sensitive to n-gradients and fluctuations
Possible extra heating
Reliable Te- control in B-field
SdH amplitude may be affected e.g. by spin splitting
SdH may be non-sinusoidal: higher harmonics
Tan, Zhu, Stormer, Pfeiffer, Baldwin, PRL 94, 016405 (2005) :

## Slide 14
Effective mass m* from SdH oscillations: side effects
Tan, Zhu, Stormer, Pfeiffer, Baldwin, PRL 94, 016405 (2005)
Physical reasons for m* variations:
Assumes Lifshitz-Kosevich formula is correct for 2DEG
Depends on LL index i
Non-parabolicity
Different models
SdH m* depends on e-e interaction

## Slide 15
MIRO is a beautiful phenomenon: access to new physics?
Amplitude vs. B  tq quantum scattering time, e.g.
Amplitude vs. B vs. B|| - tq in B||
Amplitude vs. T scattering mechanism
Amplitude vs. T  scattering mechanisms
Waveform  access to LL shape
Precise MIRO positions  m*
(B  10mT, precise B - calibration needed)
Shi, Zudov, Studenikin, Baldwin, Pfeiffer, West (2015)
Dmitriev, Mirlin, Polyakov, Zudov, Rev. Mod. Phys. 84, 1709 (2012):

## Slide 16
16
Hatke, Zudov, Pfeiffer, West, PRL 102, 066804 (2009)
No signature of the inelastic contribution
Example of MIRO T-dependence at 1K<T<4K, m=1.3107 cm2/Vs

## Slide 17
17
Shi, Zudov, Studenikin, Baldwin, Pfeiffer, West (2015)
Example of MIRO T-dependence at 0.35K<T<1.7K, m>3107 cm2/Vs

## Slide 18
Can MIRO be used for precise measurements of m* at large LL?
Hatke, MZ, Watson, Manfra, Pfeiffer, West, PRB 87, 161307(R) (2013)
What kind of m* :
Band parameter (CR)
Modified by e-e exchange interaction
Else?
?
m*MPR = 0.066
m*MIRO= 0.059
Notes: m_MIRO=0.059 was reported

## Slide 19
Example of MIROs on m~3x107 sample
Many MIRO harmonics observed, but very small field => limited by magnet precision…

## Slide 20
Sample: n=3.2 x 1011 cm2, m3107 cm2/Vs, tq=46 ps, mq=1.2106 cm2/Vs
AlxGa1-xAs/GaAs/AlGaAs QW
Width 30 nm, x=0.24
Symmetrically doped on both sides
Spacers - 80 nm,
Distance to the surface - 195 nm
Cooling process (~2h) under illumination by a red LED (i=50 mA), illumination stopped at 25K
n=3.2x1011 (EF=11.4meV)
m*(E1+Ef)=0.06793

## Slide 21
Self-consistent calculations of m*
Following: Vurgaftman et al., JAP 89, 5815 (2001)
Notes: D:\QuantumNanolab\2014\Z1-MIRO\OPJ Files\QuantumCodesmCalculation.OPJ*(Graph1)

## Slide 22
Self-consistent calculations of m* vs. E
Emax-en/e0e
Notes: D:\QuantumNanolab\2014\Z1-MIRO\OPJ Files\QuantumCodesmCalculation.OPJ*(Graph1)

## Slide 23
Chip holder for DPPH+MIRO experiment
RuO2 Thermo-resistor:
LakeShore RX-102A-BR
DPPH C18H12N5O6
(1,1-Diphenyl-2-picrylhydrazyl, Free Radical)
g*=2.0036
J. Krzystek, A. Sienkiewicz, L. Pardi, and L. C. Brunel, "DPPH as a Standard for High-Field EPR," Journal of Magnetic Resonance, vol. 125, pp. 207-211, 1997.

## Slide 24
Chip and MW antenna arrangement for MIRO experiment

## Slide 25
MIRO Frequency dependence excited by an antenna
Notes: MIROs&SdH D:\QuantumNanolab\2014\Z1-MIRO\OPJ Files\CalculatingMfromDPPH&MIRO.OPJ*(Graph11)

## Slide 26
DPPH resonance from 5 to 70 mT, T=300mK
At B=10 mT gmBB=1.16 meV=13 mK
g*=2.0036
T=300mK => ( n/n=1-exp(-g*mBB/kBT)  4%
dR/dB
d2R/dB2

## Slide 27
B-field calibration using DPPH resonance from 5 to 70 mT
90° Angle was optimized by maximizing VHall to the fifth digit.
Notes: D:\QuantumNanolab\2014\Z1-MIRO\Calculating M from DPPH&MIRO.OPJ*(Graph1)

## Slide 28
MIRO vs 1/BIPS and 1/BDPPH

## Slide 29
m* from MIRO and DPPH
Measured m*=0.0649, Theory: m*(E1+Ef)=0.06793
Notes: D:\QuantumNanolab\2014\Z1-MIRO\OPJ Files\CalculatingMfromDPPH&MIRO.OPJ*(Graph15)

## Slide 30
Measured m*=0.0649, band theory m*=0.06793
(0.0649/0.0679)=17°

## Slide 31: Electron effective mass in an ultra-high mobility GaAs/AlGaAs quantum well from MIROs and EPR experiment on DPPH
Conclusion
Measured m*MIRO= 0.0649 is smaller than theoretically calculated m*theory=0.0679
Question
is m*MIRO sensitive to e-e interactions? Or else?
Notes: In this talk I will share our experience in stabilizing a particular kind of devices – lateral SiGe QDs.